## Slide 1: Projektovanje tehnologije zavarivanja

## Slide 2: Pipeline fabrication
Pipelines is used for coveyance of fluids (liquids and gases).
Two types of pipelines exist: magistral pipelines and pipelines inside industrial facilities.

## Slide 3
Pipeline manufacturing comprises of:
Pipe fabrication
Pipeline accessories
Pipeline continuation

## Slide 4: Pipe fabrication
Welded pipes (non-seamless) are fabricated by:
Press plate bending
Spiral pipe forming

## Slide 5
Press plate bending:
With one weld seam
With two weld seams

## Slide 6
1. With one weld seam
The process of plate bending with one weld seam on a press:
a) Rolling-bending of plate edges
b) Bending of the plate central section
c) Finishing with upper mold
1 - plate

## Slide 7
Phases:
Mechanised fabrication line for welded pipelines with rollers:
1 - plate

## Slide 8
2. With two weld seams:
The process of plate bending with two weld seams:
1-plate

## Slide 9
Phases:
Mechanised fabrication line for welded pipelines with rollers and the press: 1 - plate

## Slide 10
* Pipe calibration:
Calibration and hydraulic testing of the welded pipe:
1-pipe
2-calibrating piston

## Slide 11
** Pipe halves positioning:
Pipe halves positioning :
pipe halves positioning in half-frames
Positioning of half-frames
side view
1 pipe-half; 2 half-frame; 3 frame arm; 4 frame rotation axis

## Slide 12
Spiral pipe forming:
It is used for large diameter pipelines.
Different pipe diameters can be obtained from the same plate width.
α=(40 – 66)o
B/D=2.35-1.25
Spiral pipe forming
1-bending device

## Slide 13
Phases:
Mechanised fabrication line for spiral pipe forming:
a-mechanized line, b-spiral forming, c-weld cross section, 1 – rolled sheet, 2-sheet compensating hang, 3-welded pipeline, 4-bending device

## Slide 14: Pipeline accessories
Rebra krutosti
Pipeline supports
Compensators

## Slide 15
Stiffening ribs:
- Stiffening ribs are used for pipelines with diameters of over 1.5 m
Pipeline stiffening ribs

## Slide 16
Pipeline supports –
used also for
compensating
heat dilatations
Roller pipeline support (diameter over 1,5 m)
Slide pipeline support: a) diameter of 0,6-1,5 m, b) diameter up to 0,6 m

## Slide 17
Compensators – head dilatation dilatation compansation

## Slide 18: Pipeline continuation
Two pipe sections continuation by welding

## Slide 19
Large pipeline bend.
Small diameter pipeline continuation (a), diameter reduction (b), flanges (c,d), branch (e) and bends (f,g,h).

## Slide 20
Pipeline welding to a pressure vessel or a plate:
Pipeline welding to a pressure vessel or a plate, fabrication steps: a-drilling, b-pressing (punching), c-welding

## Slide 21
Branch and diameter reduction element fabrication:
Branch and diameter reduction element fabrication

## Slide 22
Hvala na pažnji!